CO-AMORPHOUS SYSTEMS KNOWLEDGE BASE (CAMS)

1. DEFINITIONS AND SCOPE

1.1 Core definition

Co-amorphous systems (CAMs) are solid materials composed of two or more low–molecular-weight components that form a single, homogeneous amorphous phase. A defining feature is molecular-level mixing in one amorphous phase rather than a simple blend of separate amorphous domains.

1.2 CAMs versus amorphous solid dispersions (ASDs)

ASDs are usually drug plus polymer systems, where polymers reduce molecular mobility and inhibit nucleation and crystal growth. CAMs are typically drug plus small-molecule co-former (or drug–drug) systems without polymer carriers; stability is commonly achieved via specific intermolecular interactions and or elevated glass transition temperature (Tg).

1.3 Common CAM categories

1. Drug–drug CAMs for fixed-dose combination concepts and synchronized dissolution behavior.

2. Drug–small-molecule CAMs using amino acids, organic acids, bases, vitamins, sweeteners, and related small co-formers to stabilize amorphous phases and tune dissolution.

3. Natural-active CAMs (food-derived or botanical actives), where polyphenols, flavonoids, phenolic acids, and alkaloids are paired with compatible co-formers to improve functional accessibility (solubility, dispersion, and potentially bioactivity expression). This direction is increasingly discussed within broader CAM reviews and solid-form design frameworks.

2) PREPARATION TECHNOLOGIES

CAM preparation aims to disrupt crystallinity and promote intimate molecular mixing, while avoiding phase separation and residual plasticizers.

2.1 Mechanical activation (milling and grinding)

Principle: mechanical energy disrupts crystal lattices and drives solid-state mixing toward an amorphous single phase.

Typical methods: vibrational milling and planetary ball milling.

Key control variables: milling time, frequency or speed, ball-to-powder ratio, filling degree, jar material, atmosphere, and humidity.

Advantages: solvent-free and compatible with heat-sensitive compounds; useful for rapid screening.

Common risks: local heating, degradation, and batch variability if energy input and humidity are not controlled.

2.2 Solvent-based routes

2.2.1 Solvent evaporation and film casting

Principle: co-dissolve components in a common solvent or co-solvent system, then remove solvent to lock in a mixed amorphous phase.

Key solvent criteria: adequate solubility for all components, volatility and removability, and appropriate polarity and hydrogen-bonding characteristics that do not promote phase separation.

Main pitfall: residual solvent or water acts as a plasticizer that lowers Tg and accelerates recrystallization.

2.2.2 Spray drying

Principle: generate droplets from a homogeneous solution and remove solvent rapidly to produce amorphous particles.

Strengths: scalability and continuous manufacturing compatibility; direct downstream processing into powders and solid dosage forms.

Critical parameters: outlet temperature, residual solvent content, feed solids, atomization conditions, and airflow. These often govern physical stability more strongly than inlet temperature alone.

2.3 Melt-based routes (melt quenching and hot-melt processing)

Principle: form a homogeneous melt or near-melt mixture and quench rapidly to prevent ordering.

Strengths: solvent-free and potentially continuous.

Constraints: thermal stability, compatible melting and viscosity behavior, and sufficient miscibility in the molten state.

2.4 Freeze-drying (lyophilization)

Principle: prepare a solution or dispersion, freeze, then sublimate solvent under vacuum to yield a porous amorphous solid.

Use cases: water-compatible systems or those solvated by mild co-solvents.

Risk: residual water strongly plasticizes amorphous phases; moisture management is essential.

2.5 Emerging and hybrid approaches

Examples include spray-freeze drying, supercritical-fluid assisted solidification, and fluid-bed routes. These can address specialized constraints but typically require formulation-specific feasibility evaluation.

2.6 Model-guided and data-driven screening

Beyond heuristic selection, CAM development is increasingly supported by quantitative screening and informatics approaches that integrate component properties, molar ratio effects, preparation method metadata, and stability and dissolution outcomes. Quantitative literature syntheses emphasize co-formability, physical stability, and dissolution performance as core attributes to model and optimize.

3. KEY ADVANTAGES AND PERFORMANCE LOGIC

3.1 Solubility and dissolution enhancement

The amorphous state has higher free energy than crystalline forms, enabling higher apparent solubility and faster dissolution. CAMs leverage this while often improving stability relative to neat amorphous drugs.

3.2 Stability improvements relative to neat amorphous drugs

Many CAMs exhibit increased Tg and reduced molecular mobility, and specific interactions can suppress nucleation and crystal growth. Reviews consistently report improved physical stability as a major differentiator of well-designed CAMs.

3.3 High active loading without polymer carriers

Because CAMs do not require high polymer fractions, they can maintain high active content and smaller dosage volume while still improving dissolution and stability, depending on the system.

3.4 Multi-component and functional synergy

Drug–drug CAMs may support fixed-dose combination strategies and coordinated dissolution. For food-derived or botanical actives, CAMs can serve as multifunctional materials platforms when paired with suitable, safe co-formers.

4. HOW TO CONFIRM A TRUE CO-AMORPHOUS SINGLE PHASE

A robust conclusion typically requires multiple orthogonal lines of evidence.

4.1 Solid-state confirmation

1. XRPD

A broad halo with absence of sharp Bragg peaks indicates amorphous character; residual peaks imply crystallinity.

2. DSC or mDSC

A single Tg is a strong indicator of a homogeneous single amorphous phase; additional transitions may indicate phase separation or residual crystallinity.

3. TGA and residual solvent or water analysis

Residual volatiles can depress Tg and bias stability comparisons; quantifying them strengthens interpretation.

4.2 Intermolecular interaction evidence

1. FTIR and Raman

Band shifts and broadening can indicate hydrogen bonding or ionic interactions.

2. Solid-state NMR

Chemical shift changes and line-shape broadening support molecular-level mixing and altered local environments.

These interaction-focused analyses are repeatedly highlighted as central to CAM stabilization rationale and interpretation.

4.3 Stability and performance linkage

Accelerated stability testing under controlled temperature and humidity, paired with periodic XRPD and DSC checks, is necessary to confirm practical stability. Dissolution testing in both simple and biorelevant media links solid-state outcomes to functional performance.

5. MECHANISTIC UNDERSTANDING OF FORMATION AND STABILITY

5.1 Intermolecular interactions as stabilizing drivers

1. Hydrogen bonding networks

Hydrogen bonds can connect components into interaction motifs that hinder self-association and ordering; specific hydrogen-bond patterns have been experimentally analyzed in representative systems.

2. Ionic pairing and salt-like behavior

Acid–base complementarity can yield ionic interactions that often enhance both stability and dissolution; studies on amino-acid co-formers highlight the assumed importance of salt formation for stability and solubility improvement.

3. Aromatic stacking and hydrophobic association

For aromatic-rich molecules, pi-related interactions and hydrophobic packing can contribute to dense disordered structures that reduce mobility and delay crystallization; these concepts are discussed within broader solid-form and interaction-framework reviews.

5.2 Thermodynamics, miscibility, and phase behavior

Single-phase CAM formation requires sufficient miscibility in the amorphous state. Even if a CAM forms initially, thermodynamic driving forces can cause amorphous–amorphous phase separation over time, which can precede recrystallization. Tg elevation is commonly used as a practical indicator of reduced mobility, but miscibility and phase behavior still require experimental verification.

5.3 Kinetic suppression of crystallization

Crystallization proceeds via nucleation and growth. CAMs suppress crystallization by reducing diffusion and molecular rearrangement (higher Tg) and by disrupting the formation and stabilization of crystal-like clusters (interaction effects).

6. PRACTICAL DEVELOPMENT GUIDELINES

6.1 Co-former selection principles

Selection is typically guided by:

1. Functional group complementarity for hydrogen bonding or ionic pairing

2. pKa alignment for acid–base interactions when salt-like stabilization is intended

3. Safety and regulatory suitability for the intended application, especially in food-related contexts

Amino acids are a well-established co-former class in CAM development, with documented improvements in stability and dissolution for multiple drug systems.

6.2 Molar ratio optimization is not optional

Quantitative and experimental studies show that optimal ratio can differ across conditions. Under humid storage, equimolar systems may outperform off-stoichiometric mixtures due to moisture-driven interaction changes and phenomena such as salt disproportionation, implying that ratio optimization should be performed under the intended storage environment.

6.3 Moisture management is central

Moisture can plasticize amorphous phases, reduce Tg, alter molecular interactions, and accelerate recrystallization. Therefore:

1. Evaluate stability under relevant relative humidity, not only dry conditions

2. Use moisture-barrier packaging and desiccants when appropriate

3. Target Tg sufficiently above storage temperature as a risk-reduction heuristic, while still verifying experimentally

6.4 Processing and downstream manufacturability

Compaction, shear, and localized heating in downstream processes can trigger crystallization. Solid-state monitoring after key unit operations is recommended to ensure the CAM state is retained.

7. APPLICATION MAP FOR YOUR PLATFORM CONTEXT

7.1 Functional target modules

1. Solubilization

Driven by amorphous free-energy elevation, microenvironmental pH effects, and ionic pairing in selected systems.

2. Antibacterial and antioxidant function (when using bioactive co-formers or natural actives)

CAMs can improve functional accessibility by improving dispersion and release kinetics; functional outcomes still depend on the intrinsic activity and stability of the active molecules in the relevant matrix.

7.2 Application scenarios relevant to food-derived actives and green materials

1. Food preservation coatings and films

Embedding CAM powders into biopolymer matrices can couple improved release with material-based protection, provided the CAM remains stable in the film-forming environment.

2. Wound dressing materials

CAMs may enable high local loading and controlled release when combined with biocompatible film or hydrogel matrices.

3. Dietary supplements and functional foods

CAMs can improve dissolution in gastrointestinal conditions and support formulation compactness, but must be aligned with safety, stability, and regulatory constraints.

These application extensions should be validated with solid-state retention tests plus performance assays under realistic use conditions.

8) RECOMMENDED KNOWLEDGE-BASE EXTENSIONS FOR MODELING AND PLATFORMIZATION

8.1 Standard record schema

Store per formulation:

component identifiers (SMILES, InChIKey), molar ratio, preparation route, drying profile, residual water or solvent, XRPD outcome, Tg, interaction evidence summary, stability protocol and outcome, dissolution metrics.

8.2 Feature engineering targets aligned with CAM literature

1. Interaction potential features: HBD and HBA counts, pKa complementarity, ionization state proxies

2. Mobility proxies: predicted Tg, melting point-related descriptors, molecular flexibility indicators

3. Polarity and packing descriptors: logP, TPSA, aromaticity-related features

These align with the emphasis in quantitative reviews on co-formability, stability, and dissolution as core targets to predict and optimize.